ASTM A789 S32750 Technical Datasheet

Prepared from ASTM A789/A789M-22

1. Basic designation

| Standard | UNS designation | Product form | Manufacturing process | Scope |
| --- | --- | --- | --- | --- |
| ASTM A789/A789M-22 | S32750 | Seamless and welded ferritic/austenitic stainless steel tubing | No filler metal added in welded tubing | General service requiring general corrosion resistance, with particular emphasis on resistance to stress corrosion cracking |

2. Chemical composition (%)

| C | Mn | P | S | Si | Ni | Cr | Mo | N | Cu | Others |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ≤0.030 | ≤1.20 | ≤0.035 | ≤0.020 | ≤0.80 | 6.0–8.0 | 24.0–26.0 | 3.0–5.0 | 0.24–0.32 | 0.50 | PREN note C: %Cr + 3.3×%Mo + 16×%N ≥ 41 |

3. Heat treatment

| Heat-treating temperature | Quench / cooling requirement |
| --- | --- |
| 1880–2060 °F [1025–1125 °C] | rapid cooling in water or by other means |

All tubes shall be furnished in the heat-treated condition. For seamless tubes, immediately following hot forming, tubes may be individually quenched in water or rapidly cooled by other means when the temperature is not less than the specified minimum solution treatment temperature.

4. Tensile and hardness properties

| Condition / size note | Tensile strength, min | Yield strength, min | Elongation, min % | Brinell HBW max | Rockwell HRC max | Vickers HV max |
| --- | --- | --- | --- | --- | --- | --- |
| Standard | 116 [800] | 80 [550] | 15 | 300 | 32 | 300 |

For tubing smaller than 1/2 in. [12.7 mm] in outside diameter, the elongation values given for strip specimens in Table 4 apply. Mechanical property requirements do not apply to tubing smaller than 1/8 in. [3.2 mm] in outside diameter or with walls thinner than 0.015 in. [0.4 mm].

5. Lot definition for continuous process or direct quench after hot forming

| Size of tube | Size of lot |
| --- | --- |
| 2 in. [50.8 mm] and over OD and 0.200 in. [5.1 mm] and over wall | Not more than 50 tubes |
| Less than 2 in. [50.8 mm] but over 1 in. [25.4 mm] OD, or over 1 in. [25.4 mm] OD and under 0.200 in. [5.1 mm] wall | Not more than 75 tubes |
| 1 in. [25.4 mm] or less in outside diameter | Not more than 125 tubes |

6. Permissible variations in dimensions

| Group | Size, outside diameter | OD variation | Average wall variation | Minimum wall over | Minimum wall under | Cut length variation | Thin-walled tubes note |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Up to 1/2 in. [12.7 mm], excl | ±0.005 [0.13] | ±15 | 30 | 0 | 1/8 [3] over / 0 under | — |
| 2 | 1/2 to 1-1/2 in. [12.7 to 38.1 mm], excl | ±0.005 [0.13] | ±10 | 20 | 0 | 1/8 [3] over / 0 under | Thin wall: <0.065 in. [1.6 mm] specified |
| 3 | 1-1/2 to 3-1/2 in. [38.1 to 88.9 mm], excl | ±0.010 [0.25] | ±10 | 20 | 0 | 3/16 [5] over / 0 under | Thin wall: <0.095 in. [2.4 mm] specified |
| 4 | 3-1/2 to 5-1/2 in. [88.9 to 139.7 mm], excl | ±0.015 [0.38] | ±10 | 20 | 0 | 3/16 [5] over / 0 under | Thin wall: <0.150 in. [3.8 mm] specified |
| 5 | 5-1/2 to 8 in. [139.7 to 203.2 mm], incl | ±0.030 [0.76] | ±10 | 20 | 0 | 3/16 [5] over / 0 under | Thin wall: <0.150 in. [3.8 mm] specified |

Special dimension notes: (1) When tubes as ordered require wall thicknesses 3/4 in. [19 mm] or over, or an inside diameter 60% or less of the outside diameter, a wider wall variation is permitted: average wall ±12.5%, or minimum wall +25.0% / -0%. (2) For tubes less than 1/2 in. [12.7 mm] in inside diameter that cannot be successfully drawn over a mandrel, average wall may vary ±15%, or minimum wall may vary +30% / -0%. (3) These cut-length tolerances apply up to and including 24 ft [7.3 m]. For longer lengths, the over-tolerances increase by 1/8 in. [3 mm] for each 10 ft [3 m] or fraction thereof over 24 ft, or 1/2 in. [13 mm], whichever is less. (4) Ovality provisions apply to thin-walled tubes; the maximum and minimum diameters at any cross section may deviate from the nominal diameter by not more than twice the OD tolerance, provided the mean diameter remains within the tolerance.

7. Required inspection and testing

| Requirement | Details |
| --- | --- |
| Manufacture | Tubing shall be made by the seamless or welded process with no filler metal added. |
| Tension tests | One specimen for lots of not more than 50 tubes; two tubes for lots of more than 50 tubes. |
| Flaring test (seamless) | One test from one end of one tube from each lot of finished tubes; minimum inside diameter expansion 10%. |
| Flange test (welded) | One test from one end of one tube from each lot of finished tubes. |
| Hardness test | Brinell or Rockwell hardness tests on specimens from two tubes from each lot. |
| Vickers alternative | For tubing <0.354 in. [9.00 mm] ID and wall <0.065 in. [1.65 mm], Vickers may be used instead of Brinell or Rockwell. |
| Reverse flattening (welded) | One reverse flattening test on a specimen from each 1500 ft [450 m] of finished tubing. |
| Hydrostatic or NDE electric test | Each tube shall be subjected to nondestructive electric test or hydrostatic test, at manufacturer option unless otherwise specified. |
| Hydrostatic formula note | In the hydrostatic test pressure calculation, 64000 (441.2) is substituted for 32000 (220.6). |
| Surface condition | All tubes shall be free of excessive mill scale, suitable for inspection. |
| Marking | Marking shall indicate whether tubing is seamless or welded and the wall designation (average wall or minimum wall). |

8. Optional supplementary requirement

| Supplementary requirement | Summary |
| --- | --- |
| S1 Pneumatic test | When specified by the purchaser, tubing shall be examined by a pneumatic test (either air underwater or pneumatic leak test) per ASTM A1016/A1016M. |

9. Purchase order description example

Example wording

ASTM A789/A789M, UNS S32750, seamless or welded tubing, OD 25.4 mm × WT 2.11 mm (or 1 in. × 0.083 in.), average wall unless minimum wall is specified, heat treated in accordance with ASTM A789 Table 2, hydrostatic test or nondestructive electric test, test report required, special requirements if any.