ASTM A249 TP304L (S30403) Engineering Technical Datasheet

Prepared from ASTM A249/A249M-18a (Reapproved 2023)

1. Basic designation

| Standard | Grade | UNS | Product forms | Manufacturing route |
| --- | --- | --- | --- | --- |
| ASTM A249/A249M-18a (Reapproved 2023) | TP304L | S30403 | Welded tube (WLD) / Heavily Cold Worked tube (HCW) | Automatic welding with no addition of filler metal; HCW requires not less than 35 % reduction in both wall and weld prior to final anneal. |

2. Chemical composition (%)

| C | Mn | P | S | Si | Cr | Ni | Mo | N | Cu |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ≤0.030 | ≤2.00 | ≤0.045 | ≤0.030 | ≤1.00 | 18.0–20.0 | 8.0–12.0 | — | — | — |

| Nb/Ta | Ti | V | Al | Other |
| --- | --- | --- | --- | --- |
| — | — | — | — | For small diameter / thin wall with many drawing passes: C max 0.040 note applies. |

3. Mechanical properties

| Condition / thickness range | Tensile strength, min | Yield strength, min | Elongation, min % | Rockwell hardness max | Vickers hardness max |
| --- | --- | --- | --- | --- | --- |
| Standard | 70 [485] | 25 [170] | 35 | B90 | 200 |

For tubing less than 0.354 in. [9.00 mm] inside diameter and tubing less than 0.065 in. [1.65 mm] wall thickness, Vickers hardness may be used instead of Rockwell hardness.

4. Heat treatment requirements

| Solutioning temperature, min or range | Quenching / note code | Requirement |
| --- | --- | --- |
| 1900 °F [1040 °C] | A | Quenched in water or rapidly cooled by other methods, at a rate sufficient to prevent reprecipitation of chromium carbides, as demonstrated by capability of passing ASTM A262 Practice E when specified. |

5. Dimensional scope and tolerance statement

| Item | Requirement / statement |
| --- | --- |
| Usual dimensional range | 1/8 in. [3.2 mm] inside diameter to 12 in. [304.8 mm] outside diameter; wall thickness 0.015 to 0.320 in. [0.4 to 8.1 mm]. |
| Other dimensions | Other dimensions may be furnished provided all other requirements of ASTM A249 are met. |
| Mechanical-property applicability | Mechanical property requirements do not apply to tubing smaller than 1/8 in. [3.2 mm] inside diameter or 0.015 in. [0.4 mm] wall thickness. |
| Dimensional tolerances | ASTM A249 does not provide a separate dedicated dimension / wall tolerance table; general tube dimensional requirements are governed by ASTM A1016/A1016M as referenced in Section 4.1. |

6. Standard required inspection and testing

| Requirement | Details |
| --- | --- |
| Product analysis | One length of flat-rolled stock or one tube shall be analyzed for each heat. |
| Reverse-bend test requirement | A 4 in. [100 mm] minimum section shall be split longitudinally 90° on each side of the weld and bent around a mandrel of maximum thickness four times the wall thickness; no cracks or overlaps permitted. |
| Reverse-bend limitation | Not applicable when specified wall is 10 % or more of specified OD, or wall thickness is 0.134 in. [3.4 mm] or greater, or OD is less than 0.375 in. [9.5 mm]; in such cases, reverse flattening per A1016/A1016M applies. |
| Tension test frequency | One specimen for lots of not more than 50 tubes; specimens from two tubes for lots of more than 50 tubes. |
| Flattening test frequency | One flattening test from each end of one finished tube, not the one used for flange test, from each lot. |
| Flange test frequency | One flange test from each end of one finished tube, not the one used for flattening test, from each lot. |
| Reverse-bend frequency | One reverse-bend test from each 1500 ft [450 m] of finished tubing. |
| Hardness test frequency | Brinell or Rockwell hardness tests on specimens from two tubes from each lot. |
| Hydrostatic or NDE electric test | Each tube shall be subjected to either the hydrostatic or the nondestructive electric test; purchaser may specify which test is used. |
| Grain size requirement | No grade-specific grain size requirement listed for this grade in ASTM A249 Section 12. |

7. Manufacture and filler metal note

| Manufacture | Filler metal statement |
| --- | --- |
| WLD: automatic welding from flat-rolled steel; HCW: welded tube cold worked in weld and wall prior to final anneal. HCW weld shall be 100 % radiographically inspected before cold work. | No filler metal shall be used in the making of the weld per ASTM A249 Sections 5.1 and 5.1.2. |

8. Purchase order description example

Example wording

ASTM A249/A249M TP304L Tube, UNS S30403, WLD or HCW, OD 25.4 mm × WT 1.65 mm, length 6000 mm, heat treated per Table 2, hydrostatic test or nondestructive electric test as specified, test report required, and any supplementary requirements specified by purchaser.

9. Grade-specific notes

• For small diameter or thin walls, or both, where many drawing passes are required, carbon maximum 0.040 % is necessary.