ASTM A688 TP316 (S31600) Engineering Technical Datasheet

Prepared from ASTM A688/A688M-15

1. Basic designation

| Standard | Grade | UNS | Product form | Scope |
| --- | --- | --- | --- | --- |
| ASTM A688/A688M-15 | TP316 | S31600 | Seamless or welded feedwater heater tube; U-bend if specified | Austenitic stainless steel feedwater heater tubes |

2. Chemical composition (%)

| C | Mn | P | S | Si | Ni | Cr | Mo | N | Cu | Ti | Al | Other |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ≤0.08 | ≤2.00 | ≤0.040 | ≤0.030 | ≤0.75 | 10.00–14.00 | 16.00–18.00 | 2.00–3.00 | — | — | — | — | — |

3. Mechanical properties

| Condition / thickness range | Tensile strength, min | Yield strength, min | Elongation in 2 in. or 50 mm, min % |
| --- | --- | --- | --- |
| Standard | 75 [515] | 30 [205] | 35 |

4. Heat treatment requirements

| General condition | Heat treating temperature | Cooling requirement |
| --- | --- | --- |
| All finished straight tubing or straight tubing ready for U-bending shall be furnished solution annealed. | 1900 °F [1040 °C] min | Rapid cooling to below 700 °F [370 °C], sufficient to prevent harmful carbide precipitation |

If heat treatment of U-bends is specified, it applies to the U-bend area plus approximately 6 in. [150 mm] of each leg beyond the tangent point. Inside surface shall be purged with protective or inert gas during heating and cooling to below 700 °F [370 °C].

5. Standard required inspection and testing

| Requirement | Details |
| --- | --- |
| Tension test | 1 specimen for lots of not more than 50 tubes; 2 tubes for lots of more than 50 tubes. |
| Hardness test | Specimens from 2 tubes from each lot. |
| Reverse bend test (welded) | 1 test specimen from each 1500 ft [460 m] of finished tubing; not applicable for specified wall ≥10% OD, wall ≥0.134 in. [3.4 mm], or OD <0.375 in. [9.5 mm], where reverse flattening per A1016/A1016M applies. |
| Flattening test | From each end of one finished tube, not the one used for flange / flaring, from each lot. |
| Flange test (welded) | From each end of one finished tube, not the one used for flattening, from each lot. |
| Flaring test (seamless) | From each end of one finished tube, not the one used for flattening, from each lot. |
| Pressure test | Each straight tube or each U-tube after bending and post-bending heat treatment: hydrostatic or pneumatic, as specified by purchaser. |
| Nondestructive electric test | Each straight tube after finish heat treatment shall be tested in accordance with A1016/A1016M. |
| Corrosion test | One 1 in. full-section sample from the smallest radius heat-treated bend, and one 1 in. full-section sample from each lot of straight tubes, in accordance with ASTM A262. |
| Hardness limit | ≤90 HRB or equivalent; no separate grain size requirement listed for this grade |

6. Supplementary requirements (when specified in purchase order)

| Supplementary requirement | Summary |
| --- | --- |
| S1 Nondestructive eddy-current test | Each finished tube, except bending if required, shall be tested by eddy current over full cross-section. |
| S2 Additional eddy-current test option | Purchaser may specify supplementary eddy current examination per standard supplementary requirements. |
| S3 Special test reports | Purchaser may request special reports on PO. |

7. Permissible variations in dimensions

| Dimension item | Requirement |
| --- | --- |
| Outside diameter tolerance | Per ASTM A1016/A1016M for straight tubes; bent U-tube portion excluded. |
| U-bend OD tolerance, R ≥ 2×D | Major or minor diameter at bent portion shall not deviate more than 10% from nominal diameter prior to bending. |
| Minimum wall tubing | +20% / -0 from specified minimum wall thickness. |
| Average wall tubing | ±10% of nominal wall thickness. |
| U-bent section wall thickness | Not less than tf = 4RT / (4R + D), where T is required wall thickness, R is centerline bend radius, D is nominal OD. |
| Straight lengths up to 24 ft [7.3 m] | +1/8 in. [3 mm], -0. |
| Straight lengths over 24 ft [7.3 m] | Additional +1/8 in. [3 mm] for each 10 ft [3 m] or fraction thereof, up to +1/2 in. [13 mm] max. |
| U-bend leg length difference | Not greater than 1/8 in. unless otherwise specified. |
| Leg spacing at tangent points | Shall not vary from (2R - specified tube OD) by more than 1/16 in. [1.5 mm]. |
| Plane of bend deviation | Shall not exceed 1/16 in. [1.5 mm]. |

8. Table 3 U-bend leg length over-tolerance

| Specified leg length | Permissible over-tolerance |
| --- | --- |
| Up to 20 ft [6 m], incl. | 1/8 in. [3.2 mm] |
| Over 20 to 30 ft [6 to 9 m], incl. | 5/32 in. [4.0 mm] |
| Over 30 to 40 ft [9 to 12.2 m], incl. | 3/16 in. [4.8 mm] |

9. Table 4 Squareness of ends tolerance

| Tube OD | Tolerance |
| --- | --- |
| Tube OD up to 5/8 in. [15.9 mm], incl. | 0.010 in. [0.25 mm] |
| Tube OD over 5/8 to 1 in. [15.9 to 25.4 mm], incl. | 0.016 in. [0.4 mm] |

10. Filler metal / welding note

| Item | Requirement / note |
| --- | --- |
| Filler metal | Not applicable for manufacture: ASTM A688 welded tubing shall be made by automatic welding process with no addition of filler metal. |

11. Purchase order description example

Example wording

ASTM A688/A688M TP316 Tube, UNS S31600, seamless or welded, OD 19.05 mm × WT 1.24 mm × Length 12000 mm, average wall (or minimum wall as specified), solution annealed, straight or U-bent as specified, hydrostatic test or pneumatic test as specified, supplementary requirements as specified, test report required.

12. Notes

Surface condition: straight tubes after final annealing shall be pickled in nitric + hydrofluoric acid and then flushed/rinsed in water; not required if bright annealed.

Marking: all tubes shall be marked with the heat number; containers/packages shall show purchaser order number, manufacturer order number, specification, seamless or welded, grade, size and wall thickness, minimum or average, number of pieces, and item number if appropriate.